## Table 1  Conductive LB films based on anion radical salts

| Material | Matrix molecule | Dopant | Conductivity (S/cm) [Activation energy] | References |
| --- | --- | --- | --- | --- |
|  | none | I2 | 0.1 [0.15 eV] | 1, 82 |
|  | none | I2 | 0.02 [0.13 eV] | 2 |
| P(C18H37)(CH3)3 TCNQ | none | I2 | 40 (optical conductivity) | 3 |
| P(C18H37)(CH3)3 TCNQ | none | I2 | 40 (optical conductivity) | 4 |
| P(C18H37)(C2H5)(CH3)2 TCNQ | none | I2 | 40 (optical conductivity) | 5 |
| NaTCNQ | p-t-butylethylacetoxy- calix[4]arene | I2 | 0.1 | 6 |
|  | none | none | 0.01 [0.3 eV] | 7, 8 |

Table 1 Continued

|  | none |  | 0.01 | 9,10 |
| --- | --- | --- | --- | --- |
| S(CH3)3(C18H37) TCNQ |  | none | 0.01 | 11 |
|  |  | none | 10-8 | 12, 83 |

## Table 2  Conductive LB films based on cation radical salts

| Material | Matrix molecule | Dopant | Conductivity (S/cm) [Activation energy] | References |
| --- | --- | --- | --- | --- |
| EDT-TTF(SC18)2 | behenic acid | I2 | 1 [0.02 eV] | 13 |
|  | none | I2 | 10-2 | 14, 15 |
| R = CH3 R = C10H R = C16 H33 | arachidic acid arachidic acid arachidic acid | I2 I2 I2 | 2.5 x 10-3 2.7 x 10-6 2.3 x 10-1 | 16, 17 16, 17 16, 17, 18 |
| R= -CO-C15H31 (HDTTF) -CS-C15H31 (HDTTTF) -CO-C18H37 (ODTTF) | none none stearic acid pentacosa-10,12-dynoic acid | I2 I2 I2 I2 | 10-2 [0.19 eV] 1 [0.09 eV] 0.02 3 x 10-3 | 19,20 21,22 23 24 |

Table 2 Continued

| -S-C18H37 -Se-C18H37 -Te-C18H37 -S-(CH2)2-OC18H37 -S-(CH2)2-OCOC15H31 -S-COC15H31 -COO-C16H33 -CS-NH-C18H37 | stearic adid stearic adid stearic adid none none none none none | I2 I2 I2 I2 I2 I2 I2 I2 | 6 x 10-3 10-3 10-7 10-5 10-5 10-2 [0.17 eV] 10-4 | 25 25 25 26 26 26 26 26 26 |
| --- | --- | --- | --- | --- |
|  | stearic acid | I2 | 8 x 10-3 | 25, 27, 28 |
| CnBEDTTTF n = 16 n = 18 | (C17H35-OC-TCNAQ) tricosanoic acid | I2 FeCl3 I2 | 1 2 1 | 29 30 31 |

Table 2 Continued

| C18EDT-PDT-TTF | C17H35-OC-TCNAQ | I | 0.3 | 29 |
| --- | --- | --- | --- | --- |
| C18-EDT-OPDT-TTF | C17H35-OC-TCNAQ | I2 | 0.1 | 29 |
|  | straric acid | I2 | 0.9 | 32 |
| TBTTTF | stearic acid | I2 | 5 x 10-2 | 33,34 |
|  | and stearic acid | I2 | 1.1 | 35 |
|  | and stearic acid | I2 | 0.4 | 36 |

Table 2 Continued

|  | none | none | 10-2 | 37 |
| --- | --- | --- | --- | --- |
| R = CO2C2H5 CO2C4H9 | none none | I2 I2 | 4 x 10-4 4 x 10-7 | 38 38 |
|  | none | I2 | 6 x 10-3 | 39 |
|  | arachidic acid | I2 | 0.23 | 95, 97 |

Table 2 Continued

|  | tricosanoic acid | I2 | 10-3 | 40 |
| --- | --- | --- | --- | --- |
|  | none EDT-TTF(SC18)2 | I2 I2 | 10-5 10-2 | 41 42 |
| R = CF3 R = OC8H17 | methyl arachidate methyl arachidate | I2 I2 | 10-4 10-2 | 43, 44 44, 45, 46 |
|  | cadmium stearirate | I2 | 10-1 | 47 |

Table 2 Continued

|  | tricosanoic acid tricosanoic acid none tricosanoic acid | I2 I2 I2 I2 | 10-3 10-3 10-6 10-5 | 48 48 49 49 |
| --- | --- | --- | --- | --- |
|  | behnic acid | I2 | 40 metallic | 50, 51, 88, 90, 91, 93, 94 |
|  | behnic acid | I2 | 2 | 50, 89, 91 94 |
|  | none | I2 | 2 x 10-2 | 52 |

## Table 3 Conductive LB films based on charge transfer complexes

| Donor | Acceptor | Conductivity (S/cm) [Activation energy] | Refernces |
| --- | --- | --- | --- |
| TMTTF | CnTCNQ |  |  |
|  | n = 18 n = 14 | 0.1 [0.08 eV] 1 | 53 54, 55 |
| BEDOTTF | C18TCNQ C14TCNQ C10TCNQ | 0.01 1 10 | 56 56 56 87, 92, 96 |
| TBTTTF | TCNQ | 0.01 | 57 |
|  |  | 40 | 58 |
| TTF | TCNQ | 5.5 | 59 |
|  | TCNQ | 10-3 [0.27 eV] | 25 |

Taable 3 Continued

| EDT-TTF(SC18)2 EDT-TTF(SC16)2 | F4TCNQ (I2 doping) F4TCNQ (I2 doping) F4TCNQ (I2 doping) | 0.05 8 x 10-3 0.25 | 60,61 61 61 |
| --- | --- | --- | --- |
| C17DMTTF | C16TCNQ | 0.5 [0.11-0.17 eV] | 62,63 |
| C16BEDTTTF | C16TCNQ | 2.5 [0.05-0.08 eV] | 64,65 |
| C16BEDTTTF C16EDT-PDT-TTF | R = CONHC18H37 R = CO2C17H35 R = SO2NHC18H37 | 0.5 5 | 66 66 |

Table 3 Continued

| HDTTF | C16TCNQ | 5 x 10-3 [0.26 eV] alternate layer | 67 |
| --- | --- | --- | --- |
|  | (I2 doping) | 0.1 alternete layer | 68 |
|  | C18TCNQ | 1 mixed layer 150 alternate layer (conductivity of Al?) | 69 |
| BEDO-TTF | CF3TCNQ | 3.7 | 70 |
|  | DDQ | 10-4 | 71 |

## Table 4  Conductive LB films based on transition metal complexes

| Material | Matrix molecule | Doping method | Conductivity (S/cm) | Refernces |
| --- | --- | --- | --- | --- |
| 1C18-Ni | arachidic acid | E a) | 0.9 | 72 |
| 2C10-Ni | arachidic acid | Br2 | 1.0 | 72 |
| 2C12-N | arachidic acid | Br2 | 0.03 | 72 |
| 2C12-Ni | none | Br2 | 0.28 | 73 |
| 2C14-Ni | arachidic acid | Br2 | 0.09 | 72 |
| 2C16-Ni | arachidic acid | Br2 | 0.05 | 72 |
| 2C18-Ni | arachidic acid | Br2 | 9 x 10-3 | 72 |
| 2C22-Ni | arachidic acid | Br2 | 2 x 10-3 | 72 |
| 2C10-Au | arachidic acid | E a) | 1.4 | 72 |
| 2C12-Au | arachidic acid | Br2 | 0.15 | 72 |
| 2C12-Au | arachidic acid | Br2 | 0.05 | 72 |
| 2C12-Au | arachidic acid | Br2 | <10-3 | 72 |
| 3C10-Ni | arachidic acid | E a) | 1.4 | 72 |
| 3C14-Ni | arachidic acid | E a) | 0.87 | 72 |
| Table 4 Continued |  |  |  |  |
| 2C14-Au | none | E a) | 40 (metallic) | 74 |
| 2C18-Au | none | E a) | 10 | 84, 85 |
| 2C18-Au | arachidic acid | E a) | 10-1 ~ 10-2 | 84, 85 |
| 3C10-Au | arachidic acid | E a) | 40 (metallic) | 75 |
| 3C14Au | arachidic acid | E a) | 19 | 72 |
| 3C16-Au | arachidic acid | E a) | 0.46 | 72 |
| 3C18-Au | arachidic acid | Ea) | 0.12 | 72 |
| 4C10-Ni | arachidic acid | Br2 | 1.6 | 72 |
| 2C10-Pd | none | E a) | 1.0 | 72 |
| 2C18-Pd | arachidic acid | E a) | 0.01 | 76 |
| 2C10-Pt | none | Br2 | 1 x 10-3 | 72 |
| 3C10-Pd | arachidic acid | E a) | 2.8 x 10-4 | 76 |
| 3C12-Pd | arachidic acid | E a) | 8.3 x 10-3 | 76 |
| 3C16-Pd | arachidic acid | E a) | 6.1 x 10-3 | 76 |
| 3C16-Pd | arachidic acid | E a) | 0.13 | 76 |
| 3C18-Pd | arachidic acid | E a) | 9.1 x 10-3 | 76 |
| (2C12)2-Ni | none | Br2 | 0.02 | 73 |
| (2C10)2-Pd | none | E a) | 5.1 | 77 |
| (2C12)2-Pd | arachidic acid | E a) | 0.45 | 77 |
| (2C14)2-Pd | arachidic acid | E a) | 0.08 | 77 |
| (2C12)2-Pt | none | Br2 | 8x10-4 | 78 |
| Table 4 Continued |  |  |  |  |
|  |  | CnPy-M |  |  |
| C14PyNi(dmit)2 | arachidic acid | E a) | 1.2 | 72 |
| C18PyNi(dmit)2 | none | I2 | 0.2 | 79 |
| C22PyNi(dmit)2 | arachidic acid | E a) | 0.32 | 72 |
| C18PyAu(dmit)2 | none | I2 | 6x10-4 | 80 |
| (C18Py)2Ni(dmit)2 | none | I2 | 0.8 | 68 |
| (C18Py)2Pd(dmit)2 | none | I2 | 6x10-4 | 80, 86 |
| (C18Py)2Pt(dmit)2 | none | I2 | 6x10-4 | 80, 86 |
| TBANi(dmit)2 | tricosanoic acid |  | 10-7 | 81 |
| (2C12)2-Ni(mnt)2 | none | Br2 | 1x10-3 | 73 |
| (2C12)2-Pt(mnt)2 | none | Br2 | 3x10-5 | 80 |

a) E: Electrochemical oxidation in aqueous LiClO4 solution